Data sheets of 
BARITMIX-1

# Contents:

Contents:	3

1. Material safety data sheet of BARITMIX-1	5

2. Technical data sheet of BARITMIX-1	9

3. Data sheet of BARITMIX-1	15

# 1. Material safety data sheet of BARITMIX-1

1.	IDENTIFICATION OF THE PREPARATION: BARITMIX-1

Product number: RBB-3100-0,00-12

1.1.	Intended use: for industrial application

1.2.	Name of the manufacturer / supplier: 	Pólus Kincs Zrt

H-2132 Göd, Kádár utca 49.

Phone: (+36 27) 530-530 Fax: (+36 27) 530-530

1.4.	Responsible person: 		László Juhász, grad. geologist

Phone: +36-30-290-5655

E-mail: juhaszlaszlo@poluskincs.hu

1.5.	Emergency telephone number:	Egészségügyi Toxikológiai Tájékoztató Szolgálat (ETTSZ)

1096 Budapest, Nagyvárad tér 2.

Phone: (36 1) 476 6464, (36 80) 201 199

2.	HAZARDS IDENTIFICATION

Non hazardous preparation.

  - Information concerning specific hazards for human and environment:

Mixture of slightly soluble substances. Barite and quartz are insoluble in water; dolomite is soluble in acids, but poses no hazards to the environment. Iron minerals are slightly soluble.

3. 	COMPOSITION / INFORMATION ON INGREDIENTS

This product contains no hazardous materials.

Description: Unclassified ground material with a grain size of 0.00 - 12 mm containing 15 - 20 % of barite.

4.	FIRST AID MEASURES

INFORMATION TO THE PHYSICIAN: No specific prescriptions. In case of ingestion the product will be excreted through the gastro-intestinal tract without causing any symptoms. Decomposition of calcite and dolomite due to gastric acid may result fever and vomiting.

4.1.	IN CASE OF INGESTION:

Measures:

- Never give anything by mouth and do not induce vomiting if the affected person is unconscious.

- Ingestion provokes no symptoms.

- If symptoms occur call a physician immediately and show him label.

4.2. 		IN CASE OF INHALATION:

Measures:

- In case of inhalation of dust move affected person into fresh air, loosen clothing and allow to rest.

- If symptoms occur, consult a physician.

4.3. 	  IN CASE OF SKIN CONTACT:

Measures:

- Remove contaminated clothes immediately.

- Wash skin with copious amount of water and soap (for at least 15 minutes).

- If symptoms occur, consult a physician.

4.4. 	IN CASE OF EYE CONTACT:

Measures:

- In case of contact with eyes flush immediately with plenty of flowing water for 15 minutes holding eyelids apart.

- If symptoms occur, consult a physician.

5.	FIRE-FIGHTING MEASURES

Not flammable!

5.1. 	Suitable extinguishing media:

Product is non combustible.

5.2.	Unsuitable extinguishing media for safety reasons:

None known.

5.3.  	Special protective equipment:

Wear the usual full-protective clothing.

5.4. 	Hazardous combustion products:

Product is non combustible.

5.5. 	Other:

Collect extinguishing water separately. Allow only pre-treated extinguishing water to enter sewage system. Product is non combustible.

6.	ACCIDENTAL RELEASE MEASURES

  - PERSONAL PRECAUTIONS:

Keep unprotected people away, allow only well trained experts wearing suitable protective clothing to abide in the field of accident.

##### ENVIRONMENTAL PRECAUTIONS:

Dispose of spillage and waste (product/packaging) in accordance with all applicable laws. Do not allow to enter sewers/ surface or ground water. Notify the respective authorities in accordance with local law in the case of environmental pollution immediately.

##### METHODS FOR CLEANING UP:

Take up mechanically (sweep up or shovel), then place into a suitable, properly labelled, well-sealed chemical waste container for disposal.  During collection, storage and disposal of dangerous wastes wear suitable personal protective equipment.

7.	HANDLING AND STORAGE

  - Handling:

- Appropriate ventilation shall be provided!

- Observe conventional hygiene precautions.

- Non flammable, non explosive preparation.

7.2	Storage:

Keep only in original tightly closed container with the proper labelling.

Store in well-ventilated and cleanable areas only.

Follow all instructions on the label.

- Always store product in bags of proper resistance to avoid dispersion of dust.

No incompatible materials known.

- EXPOSURE CONTROLS AND PERSONAL PROTECTION

8.1. 	Engineering measures:

When using do not eat or smoke.

Use only under conventional conditions, and if adequate ventilation is provided.

Provide showers near to the workplace.

Do not inhale dust.

Provide showers and washing facilities near to the workplace.

8.2. 	Occupational exposure limits:

Other inert dusts: 10 mg/m3 (total, respirable); 5 mg/m3 (respirable)

In case of a hazardous material with no controlled concentration limit it is the employer’s duty to keep concentration levels down to a minimum achievable by existing scientific and technological means, where the hazardous substance poses no harm to workers according to the Article (6) §. 6. of the Common order the Ministers of Health and Family and Social Questions No. 25/2000 (IX. 30).

8.3. 	Personal protective equipment:

1. 	Respiratory protection: suitable dust mask.

2.   Skin protection: suitable work clothes.

3. 	Hand protection: suitable gloves according to the relevant standards.

4. 	Eye protection: suitable goggles to protect against dust.

9.	PHYSICAL AND CHEMICAL PROPERTIES:

9.1. 	Physical properties:

1. 	Physical state: unclassified ground material with a grain size of 0.00 - 12 mm

2. 	Colour: black - dark grey

3. 	Odour: rock dust like

4. 	Melting point: -

5. 	Density (20 °C): 3 g/cm3

6. 	Solubility/Miscibility: poorly miscible with water

7. 	Boiling point: -

8. 	Viscosity (cinematic at 20 oC): -

9.	Ignition temperature: -

10.	Flash point: -

11.  Auto-ignition temperature: non combustible

  - Chemical properties:

1.    pH - value (20 oC): neutral

10.	STABILITY AND REACTIVITY

10.1  	Stability:

At normal temperature: at general conditions of work: stabile.

Hazardous decomposition products: At elevated temperatures oxides of sulphur may be generated.

3.  	Hazardous reactions, materials to avoid: Unknown.

11.	TOXICOLOGICAL INFORMATION

11.1.	Acute toxicity (LD50):

No data available.

11.2. 	Other:

Product does not pose health hazards under normal conditions of use or it is unlikely that larger amounts arrive in the organism through the known routes of exposure.

Skin: Causes no irritation after short exposure.

Eyes: Causes no irritation after short exposure.

Sensitization: No sensitizing effect known.

12. 	ECOLOGICAL INFORMATION

Do not enter into drains, surface- and ground water and soil. The product is a mixture of inert and non-hazardous substances, which will be deposited by water.

Mobility: no data available.

Persistence and biodegradability: no data available.

Bioaccumulation potential: no data available.

13.     	DISPOSAL AND ELIMINATION

Disposal should be done in accordance with federal, state and local environmental control regulations.

Product: Recycling possible.

Packaging: Observe disposal consideration of packaging materials.

14.	TRANSPORT INFORMATION

No dangerous good in sense of the transport regulations.

14.1.  	Land transport:

1.  ADR/RID Class: -

2.  UN Number: -

3.  Packaging class: -

  - Marine transport:

1.  IMDG Class: -

2.  UN Number: -

3.  Packaging class: -

4.  Marine pollutant: -

14.3.  	Air transport:

ICAO/IATA: -

UN Number: -

3.  Packaging class: -

- REGULATORY INFORMATION

15.1.	Labelling:

Hazard symbol: No hazard symbol required.

Risk phrases: -

Safety phrases: -

15.2.	Restrictions on use:

No specific prescriptions.

15.3.  	National and EU regulations:

1.  Regulations on dangerous materials.

2.  Regulations on dangerous wastes.

- Regulations on water pollution.

4.  Regulations on safety.

16.  	OTHER INFORMATION

For professional or industrial use only.

Relevant R-Phrases (number and full text) of Section 2: -

This safety data sheet is formed according to the documents provided by the producer and meets the relevant regulations.

The above information is based on the present state of our knowledge and is believed to be accurate and represents the best information currently available to us, but does not purport to be all-inclusive and shall be used only as a guide.  Some other considerations being not covered by this section could be considered under given circumstances during the application and handling of the product. We make no warranty of merchantability or any other warranty, express or implied with respect to such information, and the producer of the product assumes no liability for any damage resulting from handling, or from contact with the above product.  Users should make their own investigations to determine the suitability of the information for their particular purposes and should verify compliance of the safety data sheet with the relevant legislation in the country of use. The user shall observe all relevant regulations on any activities with the given product.

# 2. Technical data sheet of BARITMIX-1

1.	IDENTITIFICATION

1.1.	IDENTIFICATION OF THE PREPARATION: BARITMIX-1

1.2.	Product number: RBB-3100-0,00-12

Name of the manufacturer / supplier: 	Pólus Kincs Zrt

H-2132 Göd, Kádár utca 49.

Phone: (+36 27) 530-530 Fax: (+36 27) 530-530

Refuse pile of Rudabánya II, converting plant

1.3.	Responsible person: 			László Juhász, grad. geologist

Phone: +36-30-290-5655

E-mail: juhaszlaszlo@poluskincs.hu

1.4.	Intended use: 				Unclassified ground material with a grain size of 0.00 - 12 mm containing 15 - 					20 % of barite for heavy concrete.

1.5.	Packaged:				In sacks in bulk, transported 80% by train, 20% on the road

2.	PROPERTIES OF THE PRODUCT

2.1.	Origin of the product:   Approximately 3.5 million tons of material with special content was piled up in the refuse pile of the ore separator of the former ore mine located on the site, plot number 099 at Rudabánya between 1965 and 1985.

2.2. 	The reserve of the mine: the reserve of the refuse pile of Rudabánya II is supposed to be 3.5 million tons.

2.3.	Quality of the material: The certificates of the material can be found in the following homepage of Pólus Kincs Zrt.: 	www.poluskincs.hu

2.4.	Description: The BARITMIX-1 product is unclassified ground material with a grain size of 0.00 - 12 mm containing 15 - 20 % of barite for heavy concrete.

2.5.	Physical properties:

1. 	Physical state: unclassified ground material with a grain size of 0.00 - 12 mm

2. 	Colour: black - dark grey

3. 	Odour: rock dust like

4. 	Melting point: -

5. 	Density (20 °C): 2.8 g/cm3

6. 	Solubility/Miscibility: poorly miscible with water

7. 	Boiling point: -

8. 	Viscosity (cinematic at 20 oC): -

9.	Ignition temperature: -

10.	Flash point: -

11.  Auto-ignition temperature: non combustible

3.           APPLICATION:

Heavy concrete: radiation protection, special technical applications requiring heavy concrete, concrete for safe and foundation.

4.            SAFETY PRECAUTIONS

  - Regulations on health: No special precaution, the product does not contain any dangerous material!

4.2. 		Fire prevention: Product is non combustible.

- OTHER INFORMATION: The detailed information of the product can be seen in the safety data sheet downloadable from the homepage of Pólus Kincs Zrt.. 
The results of the test of the materials are the followings:
5.1. Test of the heavy concrete: The results of the test of the heavy concrete made of this product are the followings:

TECHNICAL AND ECONOMIC UNIVERSITY OF BUDAPEST (МО: FI 23344)

FACULTY OF CONSTRUCTION EGINEER

TEST LABORATORY OF THE DEPARTMENT OF CONSTRUCTION MATERIALS AND ENGINEERING GEOLOGY

The laboratory is accredited by the National Committee of Accreditation and registered by the number of  NAT - 1 - 1258 / 2007.

TEST RECORD

on  compression strength of concrete

№: I - 228 / 2007.

| Customer: | PÓLUS KINCS ZRT H-2132 Göd, Kádár utca 49 | This record has 2 numbered pages |
| --- | --- | --- |
| Identification and mark of the sample: | Cube, the length of each side is 150 mm |
| Condition of the sample at the time of reception: | ----- |
| Way of sampling: | Samples taken from test mixing |
| Place of sampling: | Test mixing Technical and Economic University of Budapest, Department of Construction Materials and Engineering Geology |
| Date of sampling: | 15th May 2007. |
| Mark of concrete given by the customer: | C30/37 - XC2, XA2 32/F2 |
| Condition of after-care (storage(: | Keep wet. |
| Condition of the surface of the sample at the time of testing: | Wet |
| Preparation of the sample: | ---- |
| Date of reception: | 15th May 2007. |
| Date of test: | 12th June 2007. |
| Related regulation: | MSZ EN 12390 - 3 : 2001. |
| Additional documents: * |  |
| Record of sampling: | Archived by numbers |
| Test sheets: | Archived by numbers |

Test results

| № | Mark given by the customer | Dimensions | Weight | Density | Collapsing | Resistance to compression | Notes |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | а | b | c |  |  | force | Individual values |  |
|  |  | mm | g | kg/m3 | kN | N/mm2 |  |
| 1. | N / 1 | 149,7 | 152,0 | 149,6 | 8960 | 2632 | 1190 | 52,3 |  |
| 2. | N / 2 | 150,8 | 150,2 | 149,7 | 8920 | 2631 | 1250 | 55,2 |  |
| 3. | N / 3 | 149,6 | 149,8 | 149,9 | 8830 | 2629 | 1240 | 55,3 |  |
| The average of the individual values of the resistance to compression and density | 2630 | 54.3 | N/mm2 |

Budapest, 19th June 2007.

Project manager 				       Head of the laboratory

* The additional documents are stored at the Test Laboratory of the Department Construction Materials and Engineering Geology, Technical and Economic University of Budapest

The test results are supposed to be valid for the tested samples.

Test records can be copied in its entirely!

№: I - 228 / 2007

TECHNICAL AND ECONOMIC UNIVERSITY OF BUDAPEST (МО: FI 23344)

DEPARTMENT OF CONSTRUCTION MATERIALS AND ENGINEERING GEOLOGY

CERTIFICATE OF COMPLIANCE OF THE TEST RESULTS OF  RESISTANCE TO COMPRESSION OF CONCRETE ACCORDING TO MSZ 4798 - 1 : 2004

| 1. INFORMATION |  |  | No. of University |
| --- | --- | --- | --- |
| Customer: | PÓLUS KINCS ZRT H-2132 Göd, Kádár utca 49 |  | Mark of the sample: I - 228 / 2007 |
| Construction: | Test mixing Technical and Economic University of Budapest, Department of Construction Materials and Engineering Geology |  | Storage of samples: mixed |
| Mark of the planned concrete | C30/37 - XC2, XA2 32/F2 | Age of concrete: | 28 days |
| Volume of the tested concrete: | ---- m3 | Nominal dimensions | 150 х 150 х 150 mm |
|  |  | Quantity: | 3 pieces |

2. EVALUATION (Detailed test results can be found in the test record)

2.1. Evaluation of the density and the extant of the resistance to compression of concrete:

Requirements for the compliance of resistance to compression::

satisfactory

Requirements for the compliance of density:

satisfactory

The results of the resistance to compression can be evaluated for the appropriateness of the density and the extent of the resistance to compression.

2.2. Evaluation of the test results of the resistance to compression (test of identification according to Point В3.2. of the standard).

Required value of the resistance to compression in case of mixed storage

Average of the measured values of  the resistance to compression

1. condition:

Variety:

Permitted variety:    (According to Point В2.1.3. of MSZ 4798 - 1 : 2004. standard)

satisfactory

2. condition:

satisfactory

On the basis of the test result the sample of concrete belongs to С30 /37 class of resistance to compression.

4. REMARKS

On the basis of the density of the samples the concrete belongs to the class of heavy concretes.

Budapest, 19th June 2007.

assistant professor - project manager 	teacher of university - head of department

Valid together with the test records №.  I - 228 / 2007.

5.2. Results of the test completed by the Institute of Chemical Research of the Hungarian Academy of Science:

Institute of Chemical Research of the Hungarian Academy of Science

TEST OF X-RAY DIFFACTION COMPLETED AFTER THE SORTING OF THE RAW MATERIALS OF THE REFUSE PILE OF RUDABÁNYA-II ON 20TH JUNE 2007. The samples were taken from 83 places of sampling

MATERIAL OF THE FRACTION QUARTZ BARITE DOLOMITE COMPOUNDS OF IRON DIMENSIONS OF THE FRACTION / % / / % / / % / / % / smaller than 0.5 mm 8 35 20 20 between 0.5 and 1.5 mm 7 12 38 22,6 bigger than 1.5 mm 8 8 48 22,6 The average is between 0.00 and 8 mm 7,66 18,33 35,33 21,55

# 3. Data sheet of BARITMIX-1

1.	IDENTITIFICATION:

BARITMIX-1
of Pólus Kincs Zrt
product number: RBB-3100-0,00-12 
originating from the converting plant of refuse pile of Rudabánya II

2.	DESCRIPTION OF THE PRODUCT:

Approximately 3.5 million tons of material with special content was piled up in the refuse pile of the ore separator of the former ore mine located on the site, plot number 099 at Rudabánya between 1965 and 1985. The BARITMIX-1 product is unclassified ground material with a grain size of 0.00 - 12 mm containing 15 - 20 % of barite for heavy concrete.

The points of the classification of the so called heavy concrete:

- the mass shall be at least 2,700 kg/m3,
- high content of barite,
- high content of iron

The fields of application of the heavy concrete:

- foundation and concreting of nuclear power plants

- construction of storages of nuclear wastes

- construction of protecting shelters, bunkers against nuclear radiation

The reserve of the refuse pile is 3,500,000 tons.

The product does not contain any dangerous material and is not flammable.

It’s packed in sacks and can be transported in bulk as well, 80% by train and 20% on the road It is dark grey coloured, rock dust-like debris.

The detailed information of the product can be found in the technical and safety data sheets.

The information can be downloaded from the following homepage of Pólus Kincs Zrt.: www.poluskincs.hu.

Webmaster - contact person:

László Juhász, grad. geologist Phone: +36-30-290-5655 E-mail: juhaszlaszlo@poluskincs.hu

# Text boxes

Chemical composition of the refuse pile containing iron ore at Rudabánya

Barite,

quartz

17%

Other

3%

Dolomite,

calcite

50%

Compounds of iron

(siderite)

30%